## Slide 1
Constrained Density Functional Perturbation Theory – Hands on
Giovanni Marini and Matteo Calandra, Phys. Rev. B 104, 144103 (2021)
Giovanni Marini and Matteo Calandra

## Slide 2
Constrained Density functional perturbation theory for photexcited insulators
Complete cDFPT framework : two different chemical potentials and electron-hole plasma distribution, no supercells.
Complete structural optimization (forces/cell optimization).
Vibrational properties (phonon dispersion)
Electron-phonon interaction (including photocarriers-photocarriers screening)
S. De Gironcoli, Phys. Rev. B 51, 6773(R) (1995)
Tangney & Fahy, PRL 82, 4340 (1999), PRB Phys. Rev. B 65, 054302 (2002)
We build on top of Refs.:
Giovanni Marini and Matteo Calandra, Phys. Rev. B 104, 144103 (2021)
How does all this framework works ?
Coupling with SSCHA, Machine-learning based MD, ab initio BOMD, CPMD
How to efficiently simulate phonon and structural dynamics at very long times ?
A. Corradini, G. Marini and M.C., npj Computational Materials 11, 151 (2025)

## Slide 3
Structural Optimization – Example: Ground state Silicon
&control
calculation = 'vc-relax'
tprnfor=.true.
tstress=.true.
pseudo_dir='../Pseudo/',
/
&system
ibrav=2, celldm(1) =10.20,
nat=2, ntyp=1,
ecutwfc=30.0
occupations="fixed",
/
&electrons
/
&ions
/
&cell
/
ATOMIC_SPECIES
Si 28.086 Si.pz-vbc.UPF
ATOMIC_POSITIONS {alat}
Si 0.00 0.00 0.00
Si 0.25 0.25 0.25
K_POINTS automatic
4 4 4 1 1 1
Input file PW_Si_GS/vc-relax.in
Perdew Zunger xc (LDA)
Fixed occupation as the ground state is insulating.

## Slide 4
Structural Optimization – Example: Ground state Silicon
Output PW_Si_GS/vc-relax.out
This is the number of valence states.
As the sistem is insulating/semiconducting, no conduction states are needed.
[Si]=[Ne] 3s2 3p2 has 4 electrons in valence, two atoms per cell=8 electrons,
4 bands (two electrons per band).
bravais-lattice index = 2
lattice parameter (alat) = 10.2000 a.u.
unit-cell volume = 265.3020 (a.u.)^3
number of atoms/cell = 2
number of atomic types = 1
number of electrons = 8.00
number of Kohn-Sham states= 4
….

## Slide 5
Structural Optimization – Example: Photoexcited Silicon
Input file PW_Si_Excited/vc-relax_twochem.in
Changes are concentrated in these two blocks
&control
calculation = 'vc-relax'
tprnfor=.true.
tstress=.true.
twochem=.true.
pseudo_dir='../Pseudo/',
/
&system
ibrav=2, celldm(1) =10.20,
nat=2, ntyp=1,
ecutwfc=30.0
nbnd=8
nbnd_cond=4
nelec_cond=0.1
occupations="smearing"
degauss_cond=0.01
degauss=0.01
smearing='gaussian'
/
&electrons
/
&ions
/
&cell
/
ATOMIC_SPECIES
Si 28.086 Si.pz-vbc.UPF
ATOMIC_POSITIONS {alat}
Si 0.00 0.00 0.00
Si 0.25 0.25 0.25
K_POINTS automatic
4 4 4 1 1 1

## Slide 6
Structural Optimization – Example: Photoexcited Silicon
Input file PW_Si_Excited/vc-relax_twochem.in
Flag activating the two chemical potentials option in pw.x
&control
calculation = 'vc-relax'
tprnfor=.true.
tstress=.true.
twochem=.true.
pseudo_dir='../Pseudo/',
/
&system
ibrav=2, celldm(1) =10.20,
nat=2, ntyp=1,
ecutwfc=30.0
nbnd=8
nbnd_cond=4
nelec_cond=0.1
occupations="smearing"
degauss_cond=0.01
degauss=0.01
smearing='gaussian'
/
&electrons
/
&ions
/
&cell
/
ATOMIC_SPECIES
Si 28.086 Si.pz-vbc.UPF
ATOMIC_POSITIONS {alat}
Si 0.00 0.00 0.00
Si 0.25 0.25 0.25
K_POINTS automatic
4 4 4 1 1 1

## Slide 7
Structural Optimization – Example: Photoexcited Silicon
Input file PW_Si_Excited/vc-relax_twochem.in
We need to include more bands as we want to populate the conduction band
&control
calculation = 'vc-relax'
tprnfor=.true.
tstress=.true.
twochem=.true.
pseudo_dir='../Pseudo/',
/
&system
ibrav=2, celldm(1) =10.20,
nat=2, ntyp=1,
ecutwfc=30.0
nbnd=8
nbnd_cond=4
nelec_cond=0.1
occupations="smearing"
degauss_cond=0.01
degauss=0.01
smearing='gaussian'
/
&electrons
/
&ions
/
&cell
/
ATOMIC_SPECIES
Si 28.086 Si.pz-vbc.UPF
ATOMIC_POSITIONS {alat}
Si 0.00 0.00 0.00
Si 0.25 0.25 0.25
K_POINTS automatic
4 4 4 1 1 1

## Slide 8
Structural Optimization – Example: Photoexcited Silicon
Input file PW_Si_Excited/vc-relax_twochem.in
We need to tell pw.x how many of these bands belong to the conduction, this means
The last four bands (5,6,7,8) belongs to the conduction.
&control
calculation = 'vc-relax'
tprnfor=.true.
tstress=.true.
twochem=.true.
pseudo_dir='../Pseudo/',
/
&system
ibrav=2, celldm(1) =10.20,
nat=2, ntyp=1,
ecutwfc=30.0
nbnd=8
nbnd_cond=4
nelec_cond=0.1
occupations="smearing"
degauss_cond=0.01
degauss=0.01
smearing='gaussian'
/
&electrons
/
&ions
/
&cell
/
ATOMIC_SPECIES
Si 28.086 Si.pz-vbc.UPF
ATOMIC_POSITIONS {alat}
Si 0.00 0.00 0.00
Si 0.25 0.25 0.25
K_POINTS automatic
4 4 4 1 1 1

## Slide 9
Structural Optimization – Example: Photoexcited Silicon
Input file PW_Si_Excited/vc-relax_twochem.in
As we transfered electrons in the conduction band, leaving holes in the valence,
The system is metallic and we need to treat the system as a metal.
In principle we can use different values for the electrons broadening (degauss_cond)
And for the holes broadening (degauss)
In the present case they are identical.
&control
calculation = 'vc-relax'
tprnfor=.true.
tstress=.true.
twochem=.true.
pseudo_dir='../Pseudo/',
/
&system
ibrav=2, celldm(1) =10.20,
nat=2, ntyp=1,
ecutwfc=30.0
nbnd=8
nbnd_cond=4
nelec_cond=0.1
occupations="smearing"
degauss_cond=0.01
degauss=0.01
smearing='gaussian'
/
&electrons
/
&ions
/
&cell
/
ATOMIC_SPECIES
Si 28.086 Si.pz-vbc.UPF
ATOMIC_POSITIONS {alat}
Si 0.00 0.00 0.00
Si 0.25 0.25 0.25
K_POINTS automatic
4 4 4 1 1 1

## Slide 10
Structural Optimization – Example: Photoexcited Silicon
Input file PW_Si_Excited/vc-relax_twochem.in
Number of electron per cell in the conduction band.
For charge conservation, the same number of holes will be put in the valence band.
&control
calculation = 'vc-relax'
tprnfor=.true.
tstress=.true.
twochem=.true.
pseudo_dir='../Pseudo/',
/
&system
ibrav=2, celldm(1) =10.20,
nat=2, ntyp=1,
ecutwfc=30.0
nbnd=8
nbnd_cond=4
nelec_cond=0.1
occupations="smearing"
degauss_cond=0.01
degauss=0.01
smearing='gaussian'
/
&electrons
/
&ions
/
&cell
/
ATOMIC_SPECIES
Si 28.086 Si.pz-vbc.UPF
ATOMIC_POSITIONS {alat}
Si 0.00 0.00 0.00
Si 0.25 0.25 0.25
K_POINTS automatic
4 4 4 1 1 1

## Slide 11
Structural Optimization – Example: Photoexcited Silicon
Output file PW_Si_Excited/vc-relax_twochem.out
Increased number of KS states including conduction states
bravais-lattice index = 2
lattice parameter (alat) = 10.2000 a.u.
unit-cell volume = 265.3020 (a.u.)^3
number of atoms/cell = 2
number of atomic types = 1
number of electrons = 8.00
number of Kohn-Sham states= 8

## Slide 12
Structural Optimization – Example: Photoexcited Silicon
Output file PW_Si_Excited/vc-relax_twochem.out
Increased number of KS states including conduction states
bravais-lattice index = 2
lattice parameter (alat) = 10.2000 a.u.
unit-cell volume = 265.3020 (a.u.)^3
number of atoms/cell = 2
number of atomic types = 1
number of electrons = 8.00
number of Kohn-Sham states= 8
---------------------------------2CHEM----------------------------------
You are performing a constrained density-functional perturbation theory
employing two chemical potentials, one for electrons and one for holes.
Please refer to:
Giovanni Marini, Matteo Calandra
Lattice dynamics of photoexcited insulators
constrained density-functional perturbation theory
Phys. Rev. B 104, 144103 (2021)
doi:10.1103/PhysRevB.104.144103
The conduction manifold is constituted by 4 bands
0.1000 electrons are placed in the conduction manifold
---------------------------------2CHEM----------------------------------
Number of conduction band states and
Number of photoexcited electrons

## Slide 13
Structural Optimization – Example: Photoexcited Silicon
Output file PW_Si_Excited/vc-relax_twochem.out
Note the appearance of a non-zero stress at the
first iteration due to the presence of photoexcited
carriers.
Computing stress (Cartesian axis) and pressure
total stress (Ry/bohr**3) (kbar) P= -4.26
-0.00002894 0.00000000 0.00000000 -4.26 0.00 0.00
-0.00000000 -0.00002894 0.00000000 -0.00 -4.26 0.00
0.00000000 0.00000000 -0.00002894 0.00 0.00 -4.26
First iteration

## Slide 14
Structural Optimization – Example: Photoexcited Silicon
Output file PW_Si_Excited/vc-relax_twochem.out
Structural minimization accomplished.
Computing stress (Cartesian axis) and pressure
total stress (Ry/bohr**3) (kbar) P= -4.26
-0.00002894 0.00000000 0.00000000 -4.26 0.00 0.00
-0.00000000 -0.00002894 0.00000000 -0.00 -4.26 0.00
0.00000000 0.00000000 -0.00002894 0.00 0.00 -4.26
Computing stress (Cartesian axis) and pressure
total stress (Ry/bohr**3) (kbar) P= -0.38
-0.00000259 0.00000000 -0.00000000 -0.38 0.00 -0.00
0.00000000 -0.00000259 -0.00000000 0.00 -0.38 -0.00
-0.00000000 -0.00000000 -0.00000259 -0.00 -0.00 -0.38
First iteration
Final iteration
CELL_PARAMETERS (alat= 10.20000000)
-0.499316644 0.000000000 0.499316644
0.000000000 0.499316644 0.499316644
-0.499316644 0.499316644 -0.000000000
ATOMIC_POSITIONS (alat)
Si -0.0000000000 -0.0000000000 0.0000000000
Si 0.2496583221 0.2496583221 0.2496583221
End final coordinates
Converged structure
Initial (Ground state) a= 2.6988 Å
Converged (Exc. State) a= 2.695114 Å
Si contracts when photoexcited.

## Slide 15
Structural Optimization – Homework
Try to reproduce the following results in
Giovanni Marini and Matteo Calandra, Phys. Rev. B 104, 144103 (2021)

## Slide 16
Electronic structure, ground state v.s. photoexcited silicon
PW_Si_Bands_Excited/
The electronic structure is obtained iusing the same procedure as usual
But using the new flags we studied before.
mpirun -n 24 pw.x -npool 4 -in scf_twochem.in > scf_twochem.out
mpirun -n 24 pw.x -npool 4 -in nscf_twochem.in > nscf_twochem.out
mpirun -n 24 bands.x -npool 4 -in bands.in > bands.out
...
the Fermi energy is 5.8489 ev
the conduction Fermi energy is 7.0813 ev
! total energy = -15.84463702 Ry
...
Valence and conduction band fermi levels.

## Slide 17
Electronic structure, ground state v.s. photoexcited silicon
Ground state
Photexcited state
Note the very small holes and electrons Fermi surfaces in the photoexcited state!
Generally very large electron and phonon momenta grids are needed to converge photoexcited calculations!

## Slide 18
cDFPT – phonon calculation
Once the flags in the pw.x scf calculation has been set for the twochem option nothing is needed in the phonon calculation.
mpirun -n 24 pw.x -npool 4 -in scf_twochem.in > scf_twochem.out
mpirun -n 24 ph.x -npool 4 -in ph_twochem.in > ph_twochem.out
si
&inputph
amass(1)= 28.086,
fildyn='dynq1',
fildvscf='dvscf',
outdir='./',
alpha_mix(1)=0.2
tr2_ph=1.0d-16,
trans=.true.,
/
0.0 0.0 0.0
The phonon input is the same as for the ground state (remember to converge k and q points) and all options
valid for the ground state in ph.x are still valid for the excited state.
PH_Si_Excited/

## Slide 19
cDFPT – phonon calculation
Pert. # 1: Fermi energy shift valence (Ry) = 0.0000E+00 -2.4489E-39
Pert. # 2: Fermi energy shift valence (Ry) = -2.0961E-18 2.5102E-39
Pert. # 3: Fermi energy shift valence (Ry) = -2.8912E-18 -4.8979E-40
Pert. # 1: Fermi energy shift conduction (Ry) = 1.8070E-20 0.0000E+00
Pert. # 2: Fermi energy shift conduction (Ry) = -5.4210E-20 5.7397E-42
Pert. # 3: Fermi energy shift conduction (Ry) = -3.6140E-20 -1.5306E-41
Ph.x output
At q=0 the Fermi shift occurs both for
Valence and conduction states.
WARNING : in espresso 7.5 a bug was introduced for systems with non-zero fermi shifts.
The bug has been corrected in version 7.5NC
The version 7.4 is also correct

## Slide 20
cDFPT – phonon calculation
Diagonalizing the dynamical matrix
q = ( 0.000000000 0.000000000 0.000000000 )
*********************************************************************
freq ( 1) = -0.436693 [THz] = -14.566520 [cm-1]
freq ( 2) = -0.436693 [THz] = -14.566520 [cm-1]
freq ( 3) = -0.436693 [THz] = -14.566520 [cm-1]
freq ( 4) = 12.556812 [THz] = 418.850152 [cm-1]
freq ( 5) = 12.556812 [THz] = 418.850152 [cm-1]
freq ( 6) = 12.556812 [THz] = 418.850152 [cm-1]
*********************************************************************
Excited state
Excited state
Diagonalizing the dynamical matrix
q = ( 0.000000000 0.000000000 0.000000000 )
**************************************************************************
freq ( 1) = -0.303738 [THz] = -10.131598 [cm-1]
freq ( 2) = -0.303738 [THz] = -10.131598 [cm-1]
freq ( 3) = -0.303738 [THz] = -10.131598 [cm-1]
freq ( 4) = 15.285581 [THz] = 509.872114 [cm-1]
freq ( 5) = 15.285581 [THz] = 509.872114 [cm-1]
freq ( 6) = 15.285581 [THz] = 509.872114 [cm-1]
**************************************************************************
Note the strong softening of the optical modes due to photoexcitation

## Slide 21
cDFPT – phonon calculation Si
Giovanni Marini and Matteo Calandra, Phys. Rev. B 104, 144103 (2021)
(a)–(c) The three sheets of the valence quasi-FS for silicon
at a PC value of 0.2 𝑒/atom (d) and (e) The two sheets of the
conduction quasi-FS at a PC value of 0.2 𝑒/atom FS

## Slide 22
cDFPT – Conclusions
Giovanni Marini and Matteo Calandra, Phys. Rev. B 104, 144103 (2021)
Remember to cite
And quantum espresso
When you use cDFPT be careful in what follows:
The code is intended to work for systems that are gapped after photoexcitation. If the gap closes
after photexcitation (usually the gap is reduced by photoexcitation) it could work, depends on what
happens exactly.
Be careful with convergence. Photoexcitation creates small Fermi surfaces and calculations
requires very dense electron and phonon momentum grids.
Forces can be used to develop machine learning potential in the presence of photoexcitation
see for example:
A. Corradini, G. Marini and M.C., npj Computational Materials 11, 151 (2025)